Fine-grain structural steels, normalised rolled steel BS1449 43EE steel plate

43EE steel plate, under BS1449 standard 43EE steel plate, under BS1449 standard, we can regard 43EE steel plate as Fine-grain structural steels, normalised rolled steel

43EE steel plate is one mainly of Fine-grain structural steels, normalised rolled steel,43EE steel plate is under BS1449 standard equivalent to DIN:43EE,which with a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of 43EE is 370 to 510Mpa

43EE steel plate Chemical analysis -% by mass*

|  | Comparison of steel grades |
| --- | --- |
| 43EE | UNE36081 | AE285KG/AE285KW |
| BS1449 | DIN1614/2 | S275N |
| MATERIALS 1.0491 | NFA 36-301 | - |
|  | UN | Fe E 275KG N |

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.40 | 0.50-1.50 | 0.030 | 0.025 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

43EE steel plate Mechanical properties

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthR m[N/mm2]transv. | Fracture Elongation[%]tr ansv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t< 16mm t >16mm | 275 265 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 -50 |
| t < 3mm t> 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm > 3mm |  |  | 24 |  |