ASTM A387CL1/A387CL2 steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels for high temperature and pressure vessels

ASTM A387CL1/A387CL2 steel plate/sheet,ASTM A387CL1/A387CL2 steel plate/sheet, under ASTM standard, we can regard A387CL1/A387CL2 steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels used for high temperature and pressure vessels.

ASTM A387CL1/A387CL2 steel grade is a kind of steel which with Cr., Mo.,Cr-Mo which is mainly used for high temperature and pressure vessels.The steel grade A387CL1/A387CL2 is according to ASTM standard .The followings are the chemical composition and mechanical properties of ASTM A387CL1/A387CL2 steel plate.

The chemical composition of steel ASTM A387CL1/A387CL2 steel by [%]

| Grades | C | Mn | S | P | Si | Cr | Ni | Cu | Mo | Nb+V+Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387 CL1 | 0.05- 0.21 | 0.55-0.80 | 0.035 max | 0.035 max | 0.15-0.40 | 050-0.80 | - | - | 0.45- 0.60 | - |
| A387 CL2 | - | - | - | - | - | - | - | - | - | - |

Mechanical properties of ASTM A387CL1/A387CL2 steel

| Grade | Permissible yield point ratio | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| A387CL1 | - | 228 | 380-550 | 22 |
| A387CL2 | - | 310 | 485-620 | 22 |