Fine-grain structural steels, normalised rolled steel ASTM-SAE A537CL1/

A633Gr.C,D steel plate

A537CL1/A633Gr.C,D steel plate, under ASTM-SAEstandard A537CL1/A633Gr.C,D steel plate, under ASTM-SAEstandard, we can regard A537CL1/A633Gr.C,D steel plate as Fine-grain structural steels, normalised rolled steel.

A537CL1/A633Gr.C,D steel plate is one mainly of Fine-grain structural steels, normalised rolled steel,A537CL1/A633Gr.C,D steel plate is under ASTM-SAEstandard equivalent to DIN:TStE355, EN:S355NL, which with a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of A537CL1/A633Gr.C,D is 4800 to 620 MPa.

| Grade | Thickness (mm) | Chemical composition %. |
| --- | --- | --- |
|  |  | C. max | Si | Mn | P. max | S. max | Cu. max | Ni. max | Cr. max | Mo. max |
| A537CL 1 | 6.00-38.10 | 0.24 | 0.15-0.50 | 0.70-1.35 | 0.035 | 0.035 | 0.35 | 0.25 | 0.25 | 0.08 |
|  | 38.11-50.80 |  |  | 1.00-1.60 |  |  |  |  |  |  |

Mechanical properties of A537Class 1

| Grade | Tensile Test |
| --- | --- |
|  | Yield Strength Ksi(N/mm2) | Tensile Strength Ksi(N/mm2) | Elongation |
|  |  |  | Test piece in(mm) | %.min |
| A537 Class 1 | 50(345)min | 70-90 (485-620) | GL=8(200) GL=2(50) | 18 22 |