Carbon and low alloy steel ASTM A572Gr42/50 steel plate

A572Gr42/50 steel plate, ASTM A572Gr42/50 steel plate, under ASTM standard, we can regard A572Gr42/50 steel plate as Carbon and low alloy steel

A572Gr42/50 steel plate is one mainly of Carbon and low alloy steel, ASTM A572Gr42,50,55,60,65 steel is high strength low alloy steel plate sheet which is widely used  in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles,excavators, loaders, bulldozers , various types of cranes, hydraulic support, coal mining machinery and equipments and other structures

| A572GR50 ASTM | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | EN 10025-2 | S355JR |
|  | JIS | SS490/SM490A |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |