EN 10083 C35 steel plate high carbon steel

C35 steel plate, EN 10083 C35 steel plate, under EN 10083 standard, we can regard C35 steel plate as high carbon steel.

C35 steel plate is one mainly of high carbon steel,the application of EN 10083 C35 steel plate is equal to JIS G4051 S35C,DIN C35,UNI C35,NFA AF55-C35 ,UNE36011 C35K and AISI 1035.

| C35 EN 10083-2 Number:1.0501 | Comparision of steel grades |
| --- | --- |
|  | JIS G 4051 | S 35 C |
|  | DIN 17200 | C 35 |
|  | NFA 33-101 | AF55-C 35 |
|  | UNI 7846 | C 35 |
|  | BS 970 | 070 M 36 |
|  | UNE 36011 | C 35 k |
|  | SAE J 403-AISI | 1035 |

Chemical Composition of C35 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C35 | 0.32-0.39 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

Mechanical Properties of C35 steel

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elon- gation A5(%) | Hardness HRC | Quenching Temperature (℃) | Benda- bility | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C35 | Rolled Annealed Water-quenched Oil quenched | 440 310 | 700 480 1845 1690 | 18 30 | 53 50 | 840 880 | Min.reco-mmended Bending radius (≤90°) | 2.0 ×t | 1.0×t |