EN10111 DD11 steel plate/sheet for stamping and cold forming steels

EN10111 DD11 steel plate/sheet,EN10111 DD11 steel plate/sheet, under EN standard, we can regard DD11 steel plate/sheet as stamping and cold forming steels.EN10111 DD11 is mainly used as stamping and cold forming steels.

EN10111 DD11 steel plate/sheet is stamping and cold forming steels,it is it is suitable for non-structural presswork and forming.This jind of steel is identical to UNI:FEP11,DIN:StW22.JIS:SPHD,BS:HR3 and so on.

| DD11 EN 10111 Number: 1.0332 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | FEP11 |
|  | DIN1614 | STW22 |
|  | NFA 36-301 | 1C |
|  | JIS G 3131 | SPHD |
|  | ASTM-SAE | A621DQ-SAE1010 |
|  | BS1449 | HR3 |
|  | UNE36.093 | AP11 |

Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| DD11 | 0.12 | -- | 0.60 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-340 |  |  | 1 S |
| t < 3mm t ≥ 3mm |  | 440 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 23 A80 24 A80 28 A5 |  |