EN10111 DD13 steel plate/sheet for stamping and cold forming steels

EN10111 DD13 steel plate/sheet,EN10111 DD13 steel plate/sheet, under EN standard, we can regard DD13 steel plate/sheet as stamping and cold forming steels.EN10111 DD13 is mainly used as stamping and cold forming steels.

EN10111 DD13 steel plate/sheet is stamping and cold forming steels,which is equivalent to UNI:FeP13, BS:HR1, NFA:3C, JIS:SPHE AK, ASTM:A621DQ and UNE:AP13 steels.

| DD13 EN 10111 Number: 1.0335 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | FEP13 |
|  | BS1449 | HR1 |
|  | NFA 36-301 | 3C |
|  | JIS G 3131 | SPHE AK |
|  | ASTM-SAE | A621DQ-SAE1006AK |
|  | UNE36.093 | AP13 |

Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| DD13 | 0.08 | -- | 0.40 | 0.030 | 0.030 |

Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-310 |  |  | 0 S |
| t < 3mm t ≥ 3mm |  | 400 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 28 A80 29 A80 33 A5 |  |