EN10025 E360 steel plate/sheet for general Construction steels

EN10025 E360 steel plate/sheet,EN10025 E360 steel plate/sheet, under EN standard, we can regard E360 steel plate/sheet for general Construction steels.EN10025 E360 steel plate/sheet is for general Construction steels.The followings are the chemical composition and the mechanical properties of EN E360 steel.E360 steel is according to EN10025 standard and it is equivalent to EN:Fe690-2,DIN17100:St70-2,NFA: A70-2 and UNI7070:Fe690 steel grades.

| E360 DIN EN 10025-2 Number: 1.0070 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 690-2 |
|  | DIN17100 | ST70-2 |
|  | NFA 35-501 | A70-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 690 |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| E360 | - | - | - | - | 0.045 | 0.045 | 0.012 |

Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 360 355 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 690-900 670-830 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 4 5 6 7 10 |  |