NFA36-231 E620D steel plate/sheet High yield strength for cold forming steels

NFA36-231 E620D steel plate/sheet,NFA36-231 E620D steel plate/sheet, under NFA standard, we can regard E620D steel plate/sheet as high yield strength steels for cold-forming steels.

NFA36-231 E620D is mainly used as high yield strength steels for cold-forming steels.The NFA36-231 E620D steel is equivalent to SEW092 QStE600TM,EN S600MC and BS 68F62 steel grades.

| E620D NFA36-231 Number:1.8969 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 600TM |
|  | EN 10149-2 | S600MC |
|  | UNI8890 | - |
|  | ASTM | - |
|  | BS1449 | 68F62 |

Chemical Composition of E620D steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max | Mo max | B max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E620D | 0.12 | 0.50 | 1.9 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.22 | 0.5 | 0.005 |

Mechnical Properties of E620D steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 600 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 650-820 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 13 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 11 |