Steel plate for for Boiler Pressure Vessel EU 113 FEE315KG,KW,KT steel

FEE315KG,KW,KT steel plate, EU 113 FEE315KG,KW,KT steel plates is a kind of material for boiler and pressure vessel steel. EU 113 FEE315KG,KW, KT steel plates is characterized by a minimum yield strength of 220 - 295 MPa and by good weldability, so FEE315KG,KW,KT steel is mainly used to  for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are EU 113 FEE315KG,KW,KT steel plate's Chemical composition and mechanical properties.

If you are looking for Chinese FEE315KG,KW,KT steel supplier, if you want to know FEE315KG,KW,KT steel price, please be free to contact us.

Chemical analysis -% by mass* (max) of FEE315KG,KW,KT steel

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P265GH | 0.08-0.2 | 0.90-1.50 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

Mechanical properties of FEE315KG,KW,KT steel

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| FEE315KG,KW,KT | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 295 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 290 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 285 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 260 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 235 | 440-570 | 21 | 27 | 34 | 40 |
|  |  |  | 220 | 430-570 | 21 | 27 | 34 | 40 |