UNI7382 FeE355KGTM steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steels

UNI7382 FeE355KGTM steel plate/sheet,UNI7382 FeE355KGTM steel plate/sheet, under UNI standard, we can regard FeE355KGTM steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steel.

UNI7382 FeE355KGTM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy.The UNI7382 FeE355KGTM steel is equivalent to DIN-SEW TStE355TM,NFA E355R, EN S355M and ASTM A572GrC steel grade.

| FeE355KGTM UNI 7382 Number:1.8823 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | StE 355 TM |
|  | NFA 36-201 | E 355 R |
|  | EN 10113-3 | S355M |
|  | BS 4360 | - |
|  | ASTM | A 572 Gr.C |

Chemical Composition

| Grade | C max | Si max | Mn max | P max | S max | N max | AL min | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | Ce min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeE355KGTM | 0.14% | 0.50% | 1.60% | 0.030% | 0.025% | 0.015% | 0.02% | 0.05% | 0.10% | 0.05% | 0.30% | 0.50% | 0.10% | 0.55% | 0.39% |

Mechanical Properties

| Grade | Nom. thick.e | Yield Strengh ReH | Tensile Strength ReH | Total Elongation A5 | ℃ | Notch Impact Energy Longitud. transverse |
| --- | --- | --- | --- | --- | --- | --- |
| FeE355KGTM | ≤16mm | ≥355MPa | 470- 630 MPa |  | +20 | ≥55 | ≥31 |
|  | ＞16mm | ≥345MPa |  |  | 0 | ≥47 | ≥27 |
|  | ≥3mm |  |  | ≥22% | -10 | ≥43 | ≥24 |
|  |  |  |  |  | -20 | ≥40 | ≥20 |