Fine-grain structural steels, normalised rolled steel UNI5867 FeE420KGN steel plate

FeE420KGN steel plate, under UNI5867 standard FeE420KGN steel plate, under UNI5867 standard, we can regard FeE420KGN steel plate as Fine-grain structural steels, normalised rolled steel FeE420KGNsteel plate is one mainly of Fine-grain structural steels, normalised rolled steel,FeE420KGN steel plate is under UNI5867 standard equivalent to EN: S420N,which with a minimum elongation of 19%.

| FeE420KGN UNI5867 MATERIAL#1.8902 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE420KG/AE420KW |
|  | EN 10111 | S420N |
|  | DIN17102 | StE420 |
|  | BS4036 | - |
|  | UN | FeE420KGN |

FeE420KGN steel plate Chemical composition -% by mass*

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.60 | 1.00-1.70 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

FeE420KGN steel Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 420 400 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t≥ 3mm |  | 520-680 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 19 |  |