General purpose structural steel

General purpose structural steel plates usually used for commercial & industrial building structure: pre-engineered buildings, pre-fabricated buildings, warehouses, car parks, workshops, sports stadiums. Structural steel plates for multi-storey steel frame structures, airport hangars, railway stations structure, shopping malls etc.. High strength low alloy heavy plates for bridge construction. Plate steel for construction of railway & road vehicle chassis.

The main steel grades of General purpose structural steel plates are:

Material #: 1.0035, 1.0037, 1.0038, 1.0116, 1.0117, 1.0044, 1.0143, 1.0144, 1.0145, 1.0045, 1.0553, 1.057, 1.0577, 1.0595,1.0596, 1.005, 1.006, 1.007

EN 10025: S185, S235JR, S235JRG2,S235J2G3, S235J2G4, S275JR, S275JO, S275J2G3, S275J2G4, S355JR, S355JO, S355J2G3, S355J2G4, S355K2G3, S355K2G4, E295, E335, E360

DIN 17100: St 33, St 37-2, RSt 37-2, St 37-3 N, St 44-2, St 44-3 U, St 44-3 N, St 52-3 U, St 52-3 N, St 50-2, St 60-2, St 70-2.

NFA 35-501: A 33, E 24-2, E 24-2 NE, E 24-4, E 28-2, E 28-3, E 28-4, E 36-2, E 36-3, E 36-4, A 50-2, A 60-2, A 70-2.

UNI 7070: Fe 320, Fe 360 B, Fe 360 D, Fe 430 B, Fe 430 C, Fe 430 D, Fe 510 B, Fe 510 C, Fe 510 D, Fe 490, Fe 590, Fe 690.

BS 4360: 40 A, 40 B, 40 D, 43 B, 43 C, 43 D, 50 B, 50 C, 50 D, 50 DD

UNE 36.080: A 310-0, AE 235 B-FN, AE 235 D, AE 275 B, AE 275 C, AE 275 D, AE 355 B, AE 355 C, AE 355 D, A 490, A 590, A 690.

ASTM: A 283 B - A 569 CQ, A 283 C - A 570 Gr. 33, A 283 D - A 36, A 578 Gr. 70, A 633 Gr. A, A 572 Gr. 50 - A 678 Gr. A, A 441.

JIS G3101: SS 330, SS 400, SS 490, SS 500.

| Material # | EN 10025 | DIN 17100 | NFA 35-501 | UNI 7070 | BS 4360 | UNE 36.080 | ASTM | JIS G3101 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1.0035 | S185 | St 33 | A 33 | Fe 320 |  | A 310-0 | A 283 B - A 569 CQ | SS 330 |
| 1.0037 | S235JR | St 37-2 | E 24-2 | Fe 360 B | 40 A |  | A 283 C - A 570 Gr. 33 |  |
| 1.0038 | S235JRG2 | RSt 37-2 | E 24-2 NE |  | 40 B | AE 235 B-FN |  |  |
| 1.0116 | S235J2G3 | St 37-3 N | E 24-4 | Fe 360 D | 40 D | AE 235 D |  |  |
| 1.0117 | S235J2G4 |  |  |  |  |  |  |  |
| 1.0044 | S275JR | St 44-2 | E 28-2 | Fe 430 B | 43 B | AE 275 B | A 283 D - A 36 | SS 400 |
| 1.0143 | S275JO | St 44-3 U | E 28-3 | Fe 430 C | 43 C | AE 275 C | A 578 Gr. 70 |  |
| 1.0144 | S275J2G3 | St 44-3 N | E 28-4 | Fe 430 D | 43 D | AE 275 D | A 633 Gr. A |  |
| 1.0145 | S275J2G4 |  |  |  |  |  |  |  |
| 1.0045 | S355JR |  | E 36-2 | Fe 510 B | 50 B | AE 355 B | A 572 Gr. 50 - A 678 Gr. A | SS 490 |
| 1.0553 | S355JO | St 52-3 U | E 36-3 | Fe 510 C | 50 C | AE 355 C | A 441 |  |
| 1.057 | S355J2G3 | St 52-3 N |  | Fe 510 D | 50 D | AE 355 D |  |  |
| 1.0577 | S355J2G4 |  |  |  |  |  |  |  |
| 1.0595 | S355K2G3 |  | E 36-4 |  | 50 DD |  |  |  |
| 1.0596 | S355K2G4 |  |  |  |  |  |  |  |
| 1.005 | E295 | St 50-2 | A 50-2 | Fe 490 |  | A 490 |  | SS 500 |
| 1.006 | E335 | St 60-2 | A 60-2 | Fe 590 |  | A 590 |  |  |
| 1.007 | E360 | St 70-2 | A 70-2 | Fe 690 |  | A 690 |  |  |