Steel plate for for Boiler Pressure Vessel EN10028 P265GH

P265GH steel plate, EN10028 P265GH steel plates is a kind of material for boiler and pressure vessel steel. EN10028 P265GH steel plates is characterised by a minimum yield strength of 185 - 265 MPa and by good weldability,so P265GH steel is mainly used to  for manufacturing boilers, pressure vessels and pipes transporting hot liquids.the following are EN10028 P265GH steel plate's Chemical composition and mechanical properties.

Chemical analysis -% by mass* (max)

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P265GH | 0.20 | 0.80-1.40 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

Mechanical properties

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P265GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 265 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 255 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 245 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 215 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 200 | 400-530 | 22 | 27 | 34 | 40 |
|  |  |  | 185 | 390-530 | 22 | 27 | 34 | 40 |