SEW092 QStE340TM steel plate/sheet for High yield strength cold forming steels

SEW092 QStE340TMsteel plate/sheet,SEW092 QStE340TM steel plate/sheet, under SEW standard, we can regard QStE340TM steel plate/sheet for high yield strength cold forming steels.

SEW092 QStE340TM is a technical delivery conditions for high yield strength cold forming steels.It is according to EN10149-2 standard.we can regard QStE340TM steel plates/sheets are low-perlite steel grades offer excellent bending, flanging, cold-borderingand folding properties in both longitudinal and transverse direction. The bending radii specified below should be observed as minimum values.

| QStE340TM SEW092 MATERIAL#1.092 | Comparison of steel grades |
| --- | --- |
|  | A 517 / A 607 / J 1392 | 045 XLK |
|  | NFA 36-231 | E 315 D |
|  | BS 1449 Sec. 1.4 | HR 43F35 |
|  | EN10149-2 | QStE340TM |

QStE340TM steel plateChemical analysis-% by  mass*

| Chemical analysis -% by mass* | C | Si | Mn | P | S 1) | Altotal | Mo | Ti | B |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | max. | max. | max. | max. | max. | min. | max. | max. | max. |  |
|  | 0,12 | 0,50 | 1,30 | 0,025 | 0,020 | 0,015 | - | 0,15 | - |  |

QStE340TM steel sheetMechanical properties

| Mechanical properties | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Min.totalelongation [%] | Smallest recommended bending radius bending angles ≤ 90� |
| --- | --- | --- | --- | --- |
| QStE340TM | 315 | 390 - 510 | L0 = 80 mm | L0= 5,65 √S0 | e1) ≤ 3 | 3 < e1)< 6 | e1) > 6 |
|  |  |  | e2) < 3 | e2) ≥ 3 | 0,25 e | 0,5 e | 1,0 e |
|  |  |  | 20 | 24 |  |  |  |