EN10025 S235J2 steel plate

S235J2 steel plate, EN10025 S235J2 steel plate, under EN10025 standard, we can regard S235J2 steel plate as Carbon and low alloy steel

S235J2 steel plate is one mainly of Carbon and low alloy steel, S235J2 steel plate would be used to built containers which can bear low temperature sea water. When customers order S235J2 steel plate from us,our mill should be roll them completely according to EN10025_2 specification, the mill would issue original Mill test certificates before taking delivery for checking

The Chemical is max composition of product analysis:

| Grade | C % | Si % | Mn % | P % | S % | N % | Cu % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S235j2 | 0.190 | - | 1.500 | 0.035 | 0.035 | - | 0.060 |

The mechanical properties steel plate

| Grade | Thickness(mm) | Min Yield (Mpa) | Tensile(MPa) | Elongation(%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| S235j2 | 8mm-100mm | 215Map-235Mpa | 360-510Mpa | 21-26% | -20 | 27J |
|  | 101mm-200mm | 195Mpa | 340-500Mpa | 22% | -20 | 27J |
|  | 201mm-400mm | 175Mpa | … | 21% | -20 | 27J |
| The min impact energy is longitudinal energy |