EN10025 S235J2G3 Carbon structural steel

EN10025 S235J2G3 steel plate, EN10025 S235J2G3 steel plate is a kind of carbon structural steel.

EN10025 S235J2G3 steel plate is characterised by a minimum yield strength of 170-235MPa and tensile strength of 340-510MPa,so S235J2G3 steel is mainly used in riveted, bolted, or welded construction of bridges and buildings.the following are EN10025 S235J2G3 steel plate's Chemical composition and mechanical properties

If you are looking for Chinese S235J2G3 steel supplier,if you want to know S235J2G3 steel price, please be free to contact us.

S235J2G3 steel Chemical analysis -% by mass

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

S235J2G3 steel Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t ≤ 16mm t > 16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |