Carbon steel plate EN 10155 S235J2W steel plate

S235J2W steel plate, EN 10155 S235J2W steel plate, under EN 10155 standard, we can regard S235J2W steel plate as Carbon steel plate, S235J2W steel plate is one mainly of Carbon steel plate, S235J2W steel plate would be used to built containers which can bear low temperature sea water. When customers order S235J2W steel plate from us, our mill should be roll them completely according to EN 10155-2 specification, the mill would issue original Mill test certificates before taking delivery for checking.

| S235J2W EN10155 | Comparison of steel grades |
| --- | --- |
|  | NFA 35-502 | NFA 35-502 |
|  | UNI | UNI |

S235J2W steel plate Chemical analysis -% by mass*

| Grades | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | N max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S235J2W | 0.13 | 0.40 | 0.20-0.60 | 0.035 | 0.035 | 0.25-0.55 | 0.40-0.80 | 0.85 | - |

S235J2W steel sheet Mechanical properties

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm | ≥235 MPa | 380-510MPa | 19% | - |
| t >16mm | ≥225 MPa |  |  |  |