EN10149 S260NC steel plate/sheet as high strength steels for cold-forming, normalised steels

EN10149 S260NC steel plate/sheet,EN10149 S260NC steel plate/sheet, under EN standard, we can regard S355NC steel plate/sheet as high strength steels for cold-forming, normalised steel.

EN10149 S260NC is mainly used as high strength steels for cold-forming,normalised steels.The EN10149 S260NC steel grade offers excellent bending,flanging cold

bordering and folding properties in both longitudinal and transverse direction.The bending radiispecified below should be observed as minimum values.

| S260NC EN 10149-3 Number:1.0971 | Comparision of steel grades |
| --- | --- |
|  | DIN | QStE260N |
|  | BS 4360 | - |
|  | ASTM | - |

Chemical Composition of EN S260NC steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S260NC | 0.16 | 0.50 | 1.2 | 0.025 | 0.02 | 0.015 | 0.09 | 0.1 | 0.15 |

Mechnical Properties of EN S260NC steel

| Nominal thickness(mm) | - | - | - |
| --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 260 | 260 | 260 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 370-490 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 30 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 24 |