JISG4051 S55C steel plate high carbon steel

S55C steel plate,JISG4051 S55C steel plate, under JISG4051 standard, we can regard S55C steel plate as high carbon steel.

S55C steel plate is one mainly of high carbon steel,is treated high technical heat treatment and it helps you make Die Plate & Plastics Die Plate much easier with good quality.It is equal to EN C55,DIN17200 C55,BS970 070M55,SAE 1055 and so on.

The equivalent standards of S55C steel

| S55C JIS G 4051 Number:1.0535 | Comparision of steel grades |
| --- | --- |
|  | EN 10083-2 | C 55 |
|  | DIN 17200 | C 55 |
|  | NFA 33-101 | AF70-C 55 |
|  | UNI 7846 | C 55 |
|  | BS 970 | 070 M 55 |
|  | UNE 36011 | C 55 k |
|  | SAE J 403-AISI | 1055 |

Chemical Composition of S55C steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| S55C | 0.52-0.60 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

Mechanical Propertities of S55C steel

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elon- gation A5 (%) | Hardness HRC | Quenching Temperature (℃) | Benda- bility | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| S55C | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.reco-mmended Bending radius (≤90°) | 3.0 ×t | 1.0×t |