STM-SAE A621DQ-SAE1008 steel plate/sheet

STM-SAE A621DQ-SAE1008 steel plate/sheet,ASTM-SAE A621DQ-SAE1008 steel plate/sheet, under ASTM standard, we can regard A621DQ-SAE1008 steel plate/sheetas stamping and cold forming steels.ASTM-SAE A621DQ-SAE1008 is mainly used as stamping and cold forming steels.

ASTM-SAE A621DQ-SAE1008 steel plate/sheetis stamping and cold forming steels,which is according to ASTM-SAE standard,and based on the different thickness,the tensile strength of A621DQ-SAE1008is 420MPa.The ASTM-SAE A621DQ-SAE1008 is also equal to DIN1614:RRSTW23, JISG3131:SPHE and EN10111:DD12 steel.

| A621DQ-SAE1008 ASTM-SAE Number: 1.0398 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | - |
|  | DIN1614 | RRSTW23 |
|  | NFA 36-301 | - |
|  | JIS G 3131 | SPHE |
|  | EN 10111 | DD12 |
|  | UNE36.093 | - |

Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| SAE1008 | 0.10 | -- | 0.45 | 0.035 | 0.035 |

Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-320 |  |  | 0 S |
| t < 3mm t ≥ 3mm |  | 420 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 25 A80 26 A80 30 A5 |  |