JIS G 3116 SG295 steel plate/sheet for gas cylinders and gas vessels

SG295 steel plate/sheet, JISG 3116 SG295 steel plate/sheet, under JIS G 3116 standard, we can regard SG295 steel plate/sheet for gas cylinders and gas vessels.

SG295 steel plate/sheet is one mainly of Steel for gas cylinders and gas vessels.JISG3116 SG295 steel is grade for gas cylinders in SG255,SG295,SG325 and SG365,which with the tensile strength of 440MPa and the yield strength of 295MPa.

Chemical composition unit%

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| SG295 | 0.20 | 0.35 | 1.00 | 0.040 | 0.040 |

Mechanical properties

| Symbol | Yield point or proof stress N/mm2 (min) | Tensile strength N/mm2 min | Elongation % min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Bending Angle | Inside radius | Test piece |
| SG295 | 295 | 440 | 26 | NO.5 in rolling direction | 180° | Thickness x 1.0 Thickness x 1.5 | No.3 in rolling direction |