Carbon and low alloy steel EN10025 SM400A/B/C steel plate

SM400A/B/C steel plate, JIS3106 SM400A/B/C steel plate, under JIS3106 standard, we can regard SM400A/B/C steel plate as Carbon and low alloy steel

SM400A/B/C steel plate is one mainly of Carbon and low alloy steel, SM400A/B/C steel plate is a structural steel grade which be used in riveted, bolted, or welded construction of bridges and buildings.It is identical to DIN:St37-3U,BS:40C,EN10025:S235J0 and Fe360C and etc

| SM400B JIS3106 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE E 360 C |
|  | DIN17100 | ST37-3U |
|  | NFA 35-501 | E24-3 |
|  | BS1449 | 40C |
|  | EN 10025-2 | S235J0 |
|  | UNI7070 | FE 360 C |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm[N/mm2]transv. | Fracture Elongation [%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |