SM520B/C steel plate, JIS3106  SM520B/C steel plate, under JIS3106 standard, we can regard  SM520B/C steel plate as Carbon and low alloy steel

SM520B/C steel plate is one mainly of Carbon and low alloy steel,  SM520B/C steel grade is a low carbon, high strength structural steel With this low carbon equivalent, it process good cold forming property. SM520B steel plates usual supplied in normalized or control rolled delivery condition

Chemical analysis -% by  mass*

| Grade | C.max | Si.max | Mn | P.max | S.max |
| --- | --- | --- | --- | --- | --- |
| SM520C | 0.2 | 0.55 | 1.6 | 0.035 | 0.035 |

Mechanical properties

| Grade | Yield point of proof stress N/mm2 min | Tensile Strength N/mm2 | Elongation |
| --- | --- | --- | --- |
|  | Thickness of steel mm | Thickness of Steel mm | thickness | Test piece | % min |
|  | ≤16 | 16-40 | ≤100 |  |  |  |
|  |  |  |  | <5 | NO.5 | 19 |
| SM520C | 365 | 355 | 520-640 | ≥5<16 | NO.1A | 15 |
|  |  |  |  | ≥16<50 | NO.1A | 19 |