JIS G 3131 SPHE steel plate/sheet for stamping and cold forming steels

JIS G3131 SPHE steel plate/sheet,JIS G3131 SPHE steel plate/sheet, under JIS standard, we can regard SPHE steel plate/sheet as stamping and cold forming steels.JIS G3131 SPHE is mainly used as stamping and cold forming steels.

JIS G3131 SPHE steel plate/sheet is stamping and cold forming steels,which under specification of JIS G3131 standard.The yield strength of SPHE is 270MPA.

Chemical composition, unit% of JIS SPHE steel

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Mn max | P max | S max |
| SPHE | 0.10 | 0.50 | 0.030 | 0.035 |

Mechanical properties of JIS SPHE steel

| Symbol | Tensile strength N/mm2 min | Elongation% min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- |
|  |  | ≥1.2 <1.6mm | ≥1.6 <2mm | ≥2 <2.5mm | ≥2.5 <3.2mm | ≥3.2 <4mm | ≥4mm |  | Bending angle | Inside Radius | Test piece |
|  |  |  |  |  |  |  |  |  |  | <3.2mm | ≥3.2 mm |  |
| SPHE | 270 | 31 | 33 | 35 | 37 | 39 | 41 | No.5 in rolling direction | - | - | - | No.3 in rolling direction |