Carbon and low alloy steel EN10025 SS490 steel plate

SS490 steel plate, JIS3101 SS490 steel plate, under JIS3101 standard, we can regard SS490 steel plate as Carbon and low alloy steel

SS490 steel plate is one mainly of Carbon and low alloy steel, SS490 steel plate is alloy steel under the EN standard which is equal to DIN17100:St52-3,EN10025:S355JR,BS:50B and UNI7070:Fe510B

| SS490/SM490A JIS3101 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | ASTM | A572GR50 |
|  | EN 10025-2 | S355JR |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrength Rm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |