Carbon and low alloy steel EN10025 St52-3N steel plate

St52-3N steel plate, under DIN17100 standard St52-3N steel plate, under DIN17100 standard, we can regard St52-3N steel plate as Carbon and low alloy steel

St52-3N steel plate is one mainly of Carbon and low alloy steel, St52-3N Steel plate according to this specification are mainly for use in welded, riveted and screwed structural components, They are not intended for heat treatment, apart from stress-relieving heat treatment and normalizing. They are usually accepted by countries from Asian.Mostly,St52-3 is equal to Q345B according to Chinese standard which are both belong to low alloy steel plates. They can be worked for statically and dynamically stressed constructions

Chemical analysis -% by mass*

| Chemical elements | C max | Si max | Mn max | P max | S max. | Nb max. | Al min | N max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.15-0.50 | 1.60 | 0.035 | 0.035 | 0.02-0.04 | 0.02 | 0.009 |

Mechanical properties

| Thickness mm | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. |
| --- | --- | --- | --- |
| 10-60 | 350 | 510 | 22 |
| 60-100 | 330 | 510 | 22 |