DIN 17102 TStE355 steel plate/sheet for fine-grain structural steels, normalised rolled steels

DIN 17102 TStE355 steel plate/sheet,DIN 17102 TStE355 steel plate/sheet, under DIN standard, we can regard TStE355 steel plate/sheet as fine-grain structural steels, normalised rolled steels.DIN 17102 TStE355 is mainly used as ine-grain structural steels, normalised rolled steels.

DIN 171022 TStE355 steel plate/sheet is ine-grain structural steels, normalised rolled steel plates/sheets specially manufactured for different types of welded constructions, from base material, resistant to heat and tough for low temperatures.And it can be used for pressure boilers, storing tanks both movable and standing, high pressure pipes, bridges, masts, tethers, etc.

| T StE 355 DIN17102 MATERIAL# 1.0456 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 355 KT |
|  | EN 10025-3 | S355NL |
| un | UN | Fe E 355 KT N |
|  | NFA36 201 | E355FP |
|  | BS4360 | 50 EE |

Chemical analysis -% by mass of DIN TStE355 steel

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.50 | 0.90-1.65 | 0.025 | 0.020 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

Mechanical properties of DIN TStE355 steel

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |