DIN 17100 st44-2 Low alloy high strength steel plate

DIN 17100 st44-2 steel plate, DIN 17100 st44-2 steel plate is a kind of Low alloy high strength steel plate.

DIN 17100 st44-2 steel plate is characterised by a minimum yield strength of 265-275MPa and tensile strength of 410-580MPa,so st44-2 steel is mainly used in riveted, bolted, or welded construction of bridges and buildings.the following are DIN 17100 st44-2 steel plate's Chemical composition and mechanical properties

If you are looking for Chinese st44-2 steel supplier,if you want to know st44-2 steel price, please be free to contact us.

st44-2 steel Chemical analysis -% by mass

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.21 | 0.21 | -- | 1.50 | 0.045 | 0.045 |

st44-2 steel Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |