A283GrA/B/C/D steel plate, ASTM A283GrA/B/C/D steel plate, under ASTM standard, we can regard A283GrA/B/C/D steel plate as Carbon and low alloy steel

A283GrA/B/C/D steel plate is one mainly of Carbon and low alloy steel, ASTM A 283Â steel covers low and intermediate tensile strength carbon steel plates for general manufacturing and constructional applications. This material is normally supplied in the rimmed or semi-killed types of steel and is particularly suitable for the economical production of assemblies requiring a considerable amount of forming. Variations in low temperature impact properties are great and these steels are not recommended for those applications requiring low temperature notch toughness

| A283C ASTM | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 360 B |
|  | DIN17100 | ST37-2 |
|  | NFA 35-501 | E24-2 |
|  | JIS3101 | SS400 |
|  | EN 10025-2 | S235JR |
|  | UNI7070 | FE 360 B |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.20 | -- | 1.40 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 235 225 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |