ASTM-SAE A572Gr50 Fine-grain structural steels, normalised rolled steel

ASTM-SAE A572Gr50 steel plate/sheet, ASTM-SAE A572Gr50 steel plate/sheet, under ASTM standard, we can regard A572Gr50 Fine-grain structural steels, normalised rolled steel. ASTM-SAE A572Gr50 steel plate/sheet is for Fine-grain structural steels, normalised rolled steel.The followings are the chemical composition and the mechanical properties of ASTM-SAE A572Gr50 steel.

| A572Gr50 ASTM-SAE MATERIAL# 1.0562 | Comparison of steel grades |
| --- | --- |
|  | UNI7382 | FeE355KG |
|  | EN 10028-3 | P355N |
|  | UNE36081 | AE355KG |
|  | DIN 1614/2 | A572Gr50 |

Chemical analysis -% by  mass*

| Grades | C | Si | Mn | Ni |
| --- | --- | --- | --- | --- |
|  | max | max | max | max |
| A572Gr50 | 0.09 | 0.5 | 1.05 | 0.9 |

Mechanical properties

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t >16mm | 470 | 560 | 24 | - |