Fine-grain structural steels, normalised rolled steel ASTM-SAE A738Gr.C

A738Gr.C/A738Gr.C steel plate

A738Gr.C steel plate, under ASTM-SAE standard A738Gr.C steel plate, under ASTM-SAE standard, we can regard A738Gr.C steel plate as Fine-grain structural steels, normalised rolled steel.

A738Gr.C steel plate is one mainly of Fine-grain structural steels, normalised rolled steel,A738Gr.C steel plate is under ASTM-SAE standard equivalent to EN: S420NL,which with a minimum fracture elongation of 19% and the tensile strength of A738Gr.C is 520 to680 MPa.

| A738Gr.C ASTM-SAE MATERIAL# 1.8912 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 420 KT |
|  | EN 10111 | S420N |
|  | DIN17102 | T StE 420 |
|  | NFA36 201 | E420FP |
|  | BS4360 | - |

A738Gr.C steel Chemical analysis -% by mass*

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.60 | 1.00-1.70 | 0.025 | 0.020 | 0.55 | 0.30 | 0.80 | 0.20 | 0.05 | 0.02 |

A738Gr.C steel Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 420 400 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t≥ 3mm |  | 520-680 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 19 |  |