UNE36011 C45K steel plate high carbon steel

C45K steel plate, UNE36011 C45K steel plate, under UNE36011 standard, we can regard C45K steel plate as high carbon steel.

C45K steel plate is one mainly of high carbon steel,UNE36011 C45K steel plate is under EN 10250-2:1999 standard,the material Number of C45K steel plate is 1.0503 and the comparison steel grades of C45K steel is JIS G 4051 S45C,DIN17200 C45,BS970 070M46,EN10083 C45 and SAE J403-AISI 1042/1045 steel.

| C45K UNE 36011 Number:1.0503 | Comparision of steel grades |
| --- | --- |
|  | JIS G 4051 | S 45 C |
|  | DIN 17200 | C 45 |
|  | NFA 33-101 | AF65-C 45 |
|  | UNI 7846 | C 45 |
|  | BS 970 | 070 M 46 |
|  | EN 10083-2 | C 45 |
|  | SAE J 403-AISI | 1042/1045 |

Chemical Composition of C45K

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C45K | 0.42-0.50 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

Mechanical Properties of C45K

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elon- gation A5(%) | Hardness HRC | Quenching Temperature (℃) | Benda- bility | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C45K | Rolled Annealed Water-quenched Oil quenched | 460 330 | 750 540 2270 1980 | 18 30 | 58 55 | 820 860 | Min.reco-mmended Bending radius (≤90°) | 2.0 ×t | 1.0×t |