Steel plate for for Boiler Pressure Vessel EN10028 P235GH

P235GH steel plate, EN10028 P235GH steel plates is a kind of material for boiler and pressure vessel steel. EN10028 P235GH steel plates is characterised by a minimum yield strength of 170-230MPa and by good weldability,so P235GH steel is mainly used to  for manufacturing boilers, pressure vessels and pipes transporting hot liquids.the following are EN10028 P235GH steel plate's Chemical composition and mechanical properties

Chemical analysis -% by  mass*

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P235GH | 0.16 | 0.35 | 0.60-1.20 | 0.025 | 0.015 | 0.012 | 0.02 | 0.3 | 0.03 | 0.08 | 0.3 | 0.02 | 0.03 | 0.02 |

Mechanical properties

| Gade | Thickness (mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KV J) (min) |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | -20℃ | 0℃ | 20℃ |
| P235GH | ≤ 16 | 235 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 16＜t ≤40 | 225 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 40＜t ≤60 | 215 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 6＜t ≤100 | 200 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 100＜t ≤150 | 185 | 350 to 480 | 24 | 27 | 34 | 40 |
|  | 150＜t ≤250 | 170 | 350 to 480 | 24 | 27 | 34 | 40 |