JIS G3101 SS400 steel plate/sheet for general purpose structural steels

JIS G3101 SS400 steel plate/sheet,JIS G3101 SS400 steel plate/sheet, under JISG3101 standard, we can regard SS400 steel plate/sheet for general purpose structural steel.

JIS G3101 SS400 is a technical delivery conditions for general purpose structural steel.JIS G3101 SS400 is a type of steel sheet under JIS standard which is used to build ship, bridge, belongs to high strength sheet. JIS G3101 SS400 is equivalent to DIN:St37-2,EN S235JR,ASTM:A283C and UNI:FE360B.

| SS400 JIS3101 | Comparision of steel grades |
| --- | --- |
|  | BS 4360 | 40(A)B |
|  | CSAG40-21 | 230 G |
|  | IS | IS 226 |
|  | JIS 3106 | SM 400 A |
|  | ISO 630 | Fe 360 B |
|  | ASTM | A 36/A 283 C |

Chemical Composition

| Grade | Chemical Composition, % by weight |
| --- | --- |
|  | C. max | Si. max | Manganese | P. max | S. max |
| SS400 | - | - | - | 0.050 | 0.050 |

Mechnical Propertites

| Grade | Yield Strength min. (Mpa) | Tensile Strength MPa | Elongation min. % | Impact Resistance min.[J] |
| --- | --- | --- | --- | --- |
|  | Thickness ＜16 mm | Thickness ≥16mm |  | Thickness ＜5mm | Thickness 5-16mm | Thickness ≥16mm |  |
| SS400 | 245 | 235 | 400-510 | 21 | 17 | 21 | - |