Carbon and low alloy steel EN10025 St37-2 steel plate

St37-2 steel plate, under DIN17100 standard St37-2 steel plate, under DIN17100 standard, we can regard St37-2 steel plate as Carbon and low alloy steel

St37-2 steel plate is one mainly of Carbon and low alloy steel, St37-2 is a type of steel sheet under EN standard which is used to build ship, bridge, belongs to high strength sheet. St37-2 is equivalent to EN:S235JR,JIS:SS400,ASTM:A283C and UNI:FE360B

| ST37-2 DIN17100 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE E 360 C |
|  | EN 10025-2 | S235JR |
|  | NFA 35-501 | E24-3 |
|  | BS1449 | 40C |
|  | JIS3106 | SM400B |
|  | UNI7070 | FE 360 C |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t ≤ 16mm t > 16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |